**The Validation data of CuCeGa alloy system.**

|  |  |  |
| --- | --- | --- |
| Alloys | *Dmax* | ref |
| Ce70Ga10Cu20 | 10 | [1] |
| Ce70Ga11Cu19 | 8 | [1] |
| Ce70Ga12Cu18 | 8 | [1] |
| Ce70Ga13Cu17 | 3 | [1] |
| Ce70Ga4Cu26 | 3 | [1] |
| Ce70Ga6Cu24 | 10 | [1] |
| Ce70Ga8Cu22 | 10 | [1] |

**The Validation data of CuZrAl alloy system.**

|  |  |  |
| --- | --- | --- |
| Alloys | *Dmax* | ref |
| Cu42.5Zr42.5Al15 | 1 | [1] |
| Cu44Zr44Al12 | 2 | [1] |
| Cu45Zr45Al10 | 5 | [1] |
| Cu45Zr48Al7 | 5 | [1] |
| Cu46.25Zr46.25Al7.5 | 7 | [1] |
| Cu46.5Zr46.5Al7 | 6 | [1] |
| Cu46Zr46Al8 | 8 | [1] |
| Cu46Zr47Al7 | 3 | [1] |
| Cu47Zr47Al6 | 6 | [1] |
| Cu48Zr48Al4 | 2 | [1] |
| Cu50Zr43Al7 | 4 | [1] |
| Cu52.5Zr42.5Al5 | 2 | [1] |
| Zr45Cu45Al10 | 3 | [1] |
| Zr46Cu46Al8 | 5 | [1] |
| Zr47Cu46Al7 | 3 | [1] |
| Zr47Cu47Al6 | 5 | [1] |
| Zr48Cu45Al7 | 5 | [1] |
| Zr50Cu40Al10 | 22 | [1] |
| Zr56Cu36Al8 | 3 | [1] |
| Zr60Cu25Al15 | 12 | [1] |
| (Zr0.5Cu0.5)92Al8 | 4 | [2] |

**Reference**

1. Zhang, T.; Long, Z.; Peng, L.; Li, Z. Prediction of Glass Forming Ability of Bulk Metallic Glasses Based on Convolutional Neural Network. *Journal of Non-Crystalline Solids* **2022**, *595*, 121846.

2. Peng, L.; Long, Z.; Zhao, M. Determination of Glass Forming Ability of Bulk Metallic Glasses Based on Machine Learning. *Computational Materials Science* **2021**, *195*, 110480.